Testing Wood-Composite Strengths

Overview:

Cutting edge research, at the University of Maine, Advanced Structures and Composites Center building, involves methods that infuse polymer resins into fabrics, wood, concrete, ceramics and other materials to produce stronger, more durable composites. These composite have been found to be extremely useful for marine, automotive, construction industries and more. Material engineers are constantly researching how to modify building materials to create more desirable properties.

Objective:

Create a stronger flour/sawdust plank composites and determine the optimum sawdust to flour ratio that produces the strongest composites.

Pre-Lab:

·  Take the pre-test (6 questions)

·  Observations

·      Classroom demonstration with dough planks (record observations)

o   Dough Planks: ________________________________________________________________________________________________________________________________

Create a wet mount and observe sawdust fibers under a microscope (record observations)

o   Sawdust under microscope:

| Sketch sawdust fibers10X | Sketch sawdust fibers 40X |
| --- | --- |

Hypothesis:

Develop a hypothesis based on your observations about how the wood fibers will increase the strength of the dough planks and what ratio of sawdust to flour would be ideal to develop the strongest planks

________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________

________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________

Materials:

Making Planks                                               	Testing the Planks

100 ml beaker                                                	Scale (digital or mechanical)

500 ml beaker                                                	Calipers

Sawdust                             	               	2 desks (same size)

Flour                                  	               	Bucket  (1/group)

Salt                                     	               	 Masses / Sand

Water

Ruler

Cookie sheet

Cooking grease/Oil

Mixing bowls (1/group)

Science Notebooks

Instructions and examples of plank recipes

| Straight Baker’s Dough | Instructions | 50/50 sawdust to flour |
| --- | --- | --- |
| 200 mL Flour 50 mL NaCl 80 mL H2O | Mix NaCl and flour in bowl. Add 80 mL H2O. Mix with spoon (add a tiny bit more H2O if necessary - 5mL at a time). Knead with hands for about five minutes. Evenly roll dough into 80 cm strand Cut into four 20 cm strands. Place on a greased pan and form into 0.5 cm thick × 3 cm wide × 20 cm long planks Cook at 150°C (300°F) for one hour. | 100 mL Flour 100 mL Sawdust 50 mL NaCl 80 mL H2O |
| 25/75 flour to sawdust |  | 75/25 flour to sawdust |
| 50 mL Flour 150 mL Sawdust 50 mL NaCl 80 mL H2O |  | 150 mL Flour 50 mL Sawdust 50 mL NaCl 80 mL H2O |

Making Planks Procedure:

- Each group is assigned a plank with a particular ratio of sawdust to flour.

- Mix the flour, salt and sawdust into a mixing bowl and add 80 mL of water.

- Stir the mixture until it rolls into a large ball.

- Place dough on lab table and roll out evenly into an 80 cm strand.

- Cut the strand into sections of 20 cm.

- Place 20 cm strands on a greased cookie sheet and form into 3cm x 20 cm x .5 cm rectangle planks.

- Teacher will cook planks at 150*C (300*F) for one hour

Experimental Design:

Describe the agreed upon experimental design for your class

________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________

________________________________________________________________________________________________________________________________________________

Once an experimental design has been established students can start mixing up their wood composite

Testing Planks Procedure:

- Number each plank (1 - 4) with a marker along with the sawdust to flour ratio.

- Determine the mass of each plank and write it in marker directly on the plank

- Make and record observations about each plank (this needs to be recorded in the results section of the activity sheet)

- Arrange two desks of the same height about 15 cm apart from each other and place a plank in-between.

- Place a 1 gallon bucket to hang from the middle of the plank

- Place the plank between the desks (2 cm on each side of the desk and the 1 gallon bucket handing directly in the middle of the tank).

- When adding additional weight, it is important to wait about 30 seconds before adding more mass and listen carefully for cracking. If you hear cracking you should wait until the plank settles before adding more mass (20 grams at a time at this point).

  - Be careful the masses do not fall on the floor once the planks break. Have students spot the masses with their hand (without touching them) at all times.

Test planks:

Describe any modification the class made to the above procedure.

________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________

________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________

Results:

Record observation (qualitative and quantitative) – make sure to mark each plank with a number, the mass and the sawdust ratio.

Plank#1_________________________________________________________________________________________________________________________________________________________________________________________________________________

Plank#2_____________________________________________________________________________________________________________________________________________________

Plank#3_____________________________________________________________________________________________________________________________________________________

Plank#4_____________________________________________________________________________________________________________________________________________________

Plank#5_____________________________________________________________________________________________________________________________________________________

Plank#6_____________________________________________________________________________________________________________________________________________________

Table results:

| Plank # | Sawdust ratio | Length (cm) | Width (cm) | Height (cm) | Volume (l*w*h) (cm3) | Mass of plank (g) | Density mass/volume (g/cm3) | Mass held by plank (g) | Stress (N) [(mass held/1000)* 9.8] | Strength ratio (mass held/mass of plank) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 |  |  |  |  |  |  |  |  |  |  |
| 2 |  |  |  |  |  |  |  |  |  |  |
| 3 |  |  |  |  |  |  |  |  |  |  |
| 4 |  |  |  |  |  |  |  |  |  |  |
| Ave. |  |  |  |  |  |  |  |  |  |  |

* Shaded columns require calculations

- Mass is determined with a digital scale or double pan balance

- Length, width and height of the plank is determined with a ruler

Width

Height

Length

- Volume is determined by multiplying length by width by height

- Density is determined by dividing the mass of the plank by volume of the plank

- The mass held by the plank is the most mass each plank held without breaking

- The strength ratio is the mass held by the plank divided by the mass of the plank itself. The higher the strength-ratio value, the better the performance of the plank.

- Pool the averages for each column with the entire class.

- When pooling the data, students could create a spreadsheet with the following columns:

  - Group number

  - Flour/ Sawdust rations

  - Length (cm)

  - Width (cm)

  - Height (cm)

  - Plank Volume (cm3)  - Example spreadsheet formula“=C2*D2*E2”

  - Mass of plank (g)

  - Density of plank (g/cm3) - Example spreadsheet formula “=G2/F2”

  - Mass held by plank (g)

  - Weight or stress (N) - Example spreadsheet formula“=(G2/1000)*9.8”

  - The last column should be labeled “Strength Ratio”: and will contain a formula to calculate the “Mass Held / Mass of Plank” ratio. - Example formula “=I2/G2 “

- Once all the data is collected and pooled, groups should work together to create a bar graph that shows the sawdust/flour ratio as the manipulated variable and the average strength ratio as the responding variable.

- As an extension, An additional graph should be created. This second graph is the group’s choice and should be used to support your final claim.

- The conclusion is one of the most important parts of the entire lab activity. It is important to make a claim, provide evidence form the results and include scientific reasoning. It is also important to address any weaknesses within the experimental design and the testing procedure of the planks and provide suggestions on how to improve the research and/or future areas of research.

CONCLUSION (outline):

Claim: ________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________

Evidence: ________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________

Scientific Reasoning: ______________________________________________________
________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________

Experimental Design Weakness: ____________________________________________ ________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________

Testing Procedure Weakness: ________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________

Improve Research: _______________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________

Future area of research: ________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________

Comprehension Questions:

- Explain why it is important to test several different planks with the same ratio of sawdust to flour? Why would you want to average the results of the strength ratios for each ratio of sawdust to flour? When is it appropriate to throw out results from one plank test and average the remaining results? Provide a clear example.

- Do you think the results of the plank testing would be different on a rainy day (high humidity) versus a warm sunny day? Explain.

- Do you think a particle composite made with small granules of sand would be stronger than the sawdust fiber composite? Why or why not?